Supplementary Material

S1. Method to determine CEC

Samples (10 g) were saturated with a buffered 1.0 M ammonium acetate (NH4-Ac) solution (250 mL). The NH4-Ac leachates were analyzed for Na, K, Ca, Mg, Fe, Mn and Al by ICP-OES. The solid was then leached with an unbuffered 1.0 M potassium chloride solution (250 mL). The final KCl leachates were analyzed for NH4-N (which is the mass concentration of N atoms present is ammonia) by colorimetry (SmartChem) and CEC values were calculated in milli-equivalents per 100 g of dry sample (meq/100 g) or centimoles of charge per kg (cmol/kg). CEC (in meq/100 g or cmol (+)/kg) was calculated using the formula:

CEC=iCi × V × 100SW × EWi    	(1)

where:

- C is the concentration (in mg/L) of each cation i measured by ICP-OES or NH4-N measured by colorimetry

- V is the final extracted volume (0.250 L)

- EW is the equivalent weight (in mg/meq) for each cation i: Ca = 20, K = 39, Na = 23, Mg = 12 and N= 14

- SW is the mass of dry sample (in g) used for the analysis (10 g)

S2. PONKCS method

The PONKCS method (Scarlett and Madsen, 2006) allows for quantification of multiple disordered phases using structureless pattern fitting. PONKCS models were prepared using XRD patterns collected from 50:50 wt% mixtures of (1) lizardite originally sourced from The University of British Columbia and NIST 676a α-Al2O3 and (2) Ca-exchanged SWy-2 montmorillonite obtained from the Clay Minerals Society Source Clay Repository and NIST 676a α-Al2O3. Unit-cell parameters and space groups were obtained from Mellini and Viti (1994) for lizardite and from Viani et al. (2002) for Ca-montmorillonite as a proxy for the Ca-saponite most commonly found in kimberlites (O’Gorman and Kitchener, 1974). Peaks for these two clay phases were fitted using the Pawley method (Pawley 1981), without reference to atomic scattering information, to refine a calibrated mass, ZM, value for the unit cell of each phase. Fundamental parameters peak fitting (Cheary and Coehlo, 1998) was used for all phases. The March-Dollase correction (March, 1932; Dollase, 1986) for preferred orientation was used to model the peaks of phlogopite. PONKCS models were calibrated to the specific geometry of our XRD and tested for accuracy and precision using a set of five weighed mixtures of synthetic kimberlites (Wang et al., In prep.).

S3. Emissions offset potential calculations

The emissions offset potential results are reported in the main text (Table 3). We used the concentrations of Mg and Ca extracted during CEC analyses and measured in the NH4-acetate leachates (in mg/L) by ICP-OES for these calculations (see section S1 above). The exchangeable Mg and Ca contents for each sample were converted from mg/L to mg/kg considering 10 g of dry sample were exchanged within 250 mL of CEC solution (see section S1). Mineral eq, the equivalent proportion (in wt.%) of either brucite [Mg(OH)2] or portlandite [Ca(OH)2] that would contain these amounts of Mg and Ca if they were present in the rock sample were then calculated using (2). We can then use brucite eq and portlandite eq for comparison with the mass abundances of these traditional reactive minerals in other ores, mine residues and different types of mineral waste.

Mineral eq= CM ×100 		(2)

Where M is the mass fraction (%) of the element in the mineral (e.g., Mg comprises 41.58 % of the mass of brucite) and C the concentration of the relevant cation in the leachate (Mg for brucite) in mg/kg.

Polyhydrated Mg-carbonates such as hydromagnesite [Mg₅(CO₃)₄(OH)₂·4H₂O] and Ca-carbonates such as calcite (CaCO3) are the most likely phases to precipitate at ambient temperature. The amounts of hydromagnesite and calcite that could be produced from the extracted Mg and Ca were calculated using equation 3. Here, the equivalent CO2 (in wt.%) stored within secondary carbonate minerals (e.g., hydromagnesite) was calculated using the mass fraction of CO2, which we name the storage factor (SF), in the mineral (0.3764 for hydromagnesite). The same calculation was done to obtain the equivalent CO2 stored within calcite (SF = 0.4397).

CO2 eq =Mineral eq ×SF		(3)

For Venetia, we considered CO2 stored in hydromagnesite only because most of the Ca likely originated from calcite dissolution. For Gahcho Kué, we considered the CO2 stored in both calcite and hydromagnesite since bedrock calcite is absent or present only in small amounts. Considering the annual tailings production (ATP) of 4.74 Mt/year at Venetia and 0.91 Mt/year at Gahcho Kué, as reported by Mervine et al. (2018), we calculated the annual mass of CO2 which could be stored (in t CO2/year) using equation 4:

Annual CO2 stored =CO2 eq×ATP	(4)

Last, the offset potential (in %) was calculated using the annual CO2 emissions (Annual CO2 em) of the two mines as reported by Mervine et al. (2018): 0.91 Mt CO2/year for Venetia and 0.084 Mt CO2 per year at Gahcho Kué, using equation 5:

Total offset potential =Annual CO2 stored ×100Annual CO2 em	(5)

TABLES

Table S1. Bulk elemental chemistry of the studied samples from Gahcho Kué and Venetia mines

| Sample | Total C | TIC | TOC | S | Al | Ba | Be | Ca | Cr | Cu | Fe | K | Li | Mg | Mn | Ni | P | Sc | Si | Sr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | % | % | % | % | % | ppm | ppm | % | ppm | ppm | % | % | ppm | % | ppm | ppm | % | ppm | % | ppm |
| 17VEN-K1-KIMB1 | 1.13 | 1.11 | 0.02 | 0.026 | 2.14 | 910 | <5 | 5 | 1370 | 30 | 6.16 | 1.5 | 20 | 17 | 1090 | 1200 | 0.16 | 16 | 16.2 | 530 |
| 17VEN-K1-KIMB2 | 0.947 | 0.93 | 0.017 | 0.026 | 1.75 | 1040 | <5 | 5.2 | 1380 | 40 | 5.66 | 1.5 | <10 | 18.1 | 1000 | 1220 | 0.18 | 15 | 17 | 750 |
| 17VEN-K1-KIMB3 | 0.633 | 0.59 | 0.043 | 0.03 | 2.12 | 870 | <5 | 5 | 1360 | 60 | 5.71 | 2.1 | 30 | 15.8 | 1140 | 1140 | 0.14 | 14 | 18.4 | 560 |
| 17VEN-K2-KIMB1 | 0.375 | 0.21 | 0.165 | 0.064 | 2.91 | 2660 | <5 | 5.6 | 730 | 70 | 6.45 | 0.9 | 20 | 13.2 | 1320 | 915 | 0.1 | 15 | 19.4 | 630 |
| 17VEN-K2-KIMB2 | 1.16 | 0.91 | 0.25 | 0.035 | 3.29 | 970 | <5 | 5.8 | 770 | 50 | 5.6 | 1.8 | 40 | 11.9 | 1420 | 646 | 0.17 | 17 | 17.9 | 610 |
| 17VEN-K3-KIMB1 | 0.552 | 0.54 | 0.012 | 0.056 | 2.3 | 1040 | <5 | 5.7 | 1070 | 50 | 5.48 | 1.8 | 40 | 16.2 | 1440 | 973 | 0.18 | 14 | 17.7 | 650 |
| 17VEN-K3-KIMB2 | 0.132 | 0.11 | 0.022 | 0.068 | 2.78 | 1030 | <5 | 6.3 | 1110 | 70 | 6.68 | 1.9 | 30 | 14.8 | 1540 | 888 | 0.19 | 19 | 18.2 | 490 |
| 17VEN-K3-KIMB3 | 0.367 | 0.31 | 0.057 | 0.046 | 2.95 | 970 | <5 | 6.2 | 790 | 70 | 6.24 | 2.6 | 30 | 13.6 | 1590 | 877 | 0.15 | 17 | 19.2 | 510 |
| 17VEN-K3-KIMB4 | 0.76 | 0.7 | 0.06 | 0.065 | 1.63 | 1080 | <5 | 6.3 | 1180 | 40 | 6.41 | 1 | <10 | 17.1 | 1900 | 977 | 0.25 | 15 | 16.4 | 760 |
| 17VEN-CRD-SampleA | 0.743 | 0.71 | 0.033 | 0.045 | 2.55 | 880 | <5 | 4.9 | 1010 | 70 | 5.78 | 1.5 | 20 | 15 | 1100 | 1060 | 0.14 | 15 | 19.1 | 560 |
| 17VEN-CRD-SampleB | 0.596 | 0.58 | 0.016 | 0.024 | 4 | 700 | <5 | 5.1 | 560 | 50 | 5.45 | 1.5 | 20 | 9.96 | 1080 | 648 | 0.11 | 17 | 20.9 | 470 |
| 17VEN-CRD1-01A | 0.863 | 0.69 | 0.173 | 0.035 | 2.55 | 910 | <5 | 5 | 1070 | 60 | 5.81 | 1.6 | 20 | 15.2 | 1110 | 1010 | 0.15 | 15 | 19.1 | 580 |
| 17VEN-FRD2-SampleA-Cycl | 0.505 | 0.41 | 0.095 | 0.048 | 3.88 | 720 | <5 | 4.2 | 590 | 60 | 5.63 | 1.8 | 20 | 10.2 | 1030 | 705 | 0.09 | 17 | 21 | 400 |
| 17VEN-FRD1-06a | 0.597 | 0.54 | 0.057 | 0.062 | 4.26 | 750 | <5 | 4.7 | 620 | 60 | 5.48 | 1.8 | 30 | 9.11 | 1250 | 550 | 0.11 | 17 | 21.5 | 390 |
| 17VEN-FRD2-11A | 0.629 | 0.59 | 0.039 | 0.114 | 3.06 | 760 | <5 | 4.4 | 740 | 50 | 5.41 | 1.3 | 20 | 13.5 | 980 | 963 | 0.11 | 12 | 18.3 | 420 |
| 17VEN-FRD2-12A | 0.702 | 0.63 | 0.072 | 0.104 | 3.06 | 820 | <5 | 4.7 | 730 | 60 | 5.62 | 1.3 | 20 | 13.9 | 990 | 1010 | 0.12 | 12 | 18.1 | 460 |
| 17VEN-FRD2-13A | 0.48 | 0.45 | 0.03 | 0.063 | 3.06 | 760 | <5 | 4.5 | 720 | 60 | 5.5 | 1.1 | 30 | 13.8 | 1020 | 953 | 0.09 | 12 | 19.6 | 430 |
| 17GK-21 | 0.11 | 0.08 | 0.03 | 0.018 | 1.55 | 1120 | <5 | 4 | 1470 | 50 | 5.59 | 1.2 | 20 | 18.8 | 1030 | 1350 | 0.14 | 10 | 17.9 | 520 |
| 17GK-22 | 0.251 | 0.24 | 0.011 | 0.063 | 1.32 | 400 | <5 | 0.9 | 1340 | 120 | 5.31 | 0.4 | 20 | 21.4 | 1060 | 1250 | 0.15 | 10 | 17 | 390 |
| 17GK-23 | 0.066 | 0.03 | 0.036 | 0.02 | 1.5 | 1230 | <5 | 2.9 | 1420 | 50 | 5.76 | 1.4 | 20 | 19 | 1020 | 1440 | 0.18 | 10 | 18 | 600 |
| 17GK-J-24 | 0.034 | <0.01 | 0.034 | 0.012 | 2.96 | 740 | <5 | 0.9 | 1120 | 60 | 4.27 | 1.3 | 100 | 15.2 | 380 | 941 | 0.08 | 8 | 19.8 | 310 |

Table S1. Continued

| Sample | Ti | V | Zn | Ag | As | Bi | Cd | Ce | Co | Cs | Dy | Er | Eu | Ga | Gd | Ge | Hf | Ho | In | La |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | % | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm |
| 17VEN-K1-KIMB1 | 0.6 | 121 | 60 | <1 | <5 | <0.1 | <0.2 | 126 | 87.6 | 3.4 | 2.31 | 1.03 | 1.59 | 7 | 4.1 | <1 | 2 | 0.44 | <0.2 | 73.4 |
| 17VEN-K1-KIMB2 | 0.59 | 73 | 51 | <1 | <5 | <0.1 | <0.2 | 143 | 81.6 | 1.7 | 2.45 | 0.91 | 1.85 | 6 | 4.54 | <1 | 2 | 0.4 | <0.2 | 84.2 |
| 17VEN-K1-KIMB3 | 0.49 | 77 | 47 | <1 | <5 | <0.1 | <0.2 | 119 | 79.5 | 3.2 | 2.22 | 0.99 | 1.45 | 8 | 3.82 | 1 | 2 | 0.38 | <0.2 | 68.5 |
| 17VEN-K2-KIMB1 | 0.39 | 104 | 68 | <1 | <5 | <0.1 | <0.2 | 78.6 | 79 | 2.3 | 2.32 | 1.2 | 1.22 | 8 | 3.33 | 1 | 2 | 0.45 | <0.2 | 43.1 |
| 17VEN-K2-KIMB2 | 0.49 | 109 | 365 | <1 | <5 | 0.1 | 1.2 | 122 | 54 | 5.5 | 3.21 | 1.59 | 1.51 | 10 | 4.7 | 1 | 3 | 0.6 | <0.2 | 74.1 |
| 17VEN-K3-KIMB1 | 0.45 | 90 | 57 | <1 | <5 | <0.1 | <0.2 | 126 | 72.3 | 2.7 | 2.39 | 1.01 | 1.6 | 7 | 4.29 | <1 | 2 | 0.43 | <0.2 | 73.2 |
| 17VEN-K3-KIMB2 | 0.63 | 146 | 81 | <1 | <5 | <0.1 | 0.3 | 134 | 71 | 3.2 | 3.66 | 1.73 | 2.03 | 8 | 5.37 | 1 | 3 | 0.67 | <0.2 | 78.7 |
| 17VEN-K3-KIMB3 | 0.47 | 110 | 102 | <1 | <5 | <0.1 | 0.3 | 105 | 66.8 | 4.5 | 2.73 | 1.31 | 1.48 | 10 | 3.95 | 1 | 3 | 0.49 | <0.2 | 62.3 |
| 17VEN-K3-KIMB4 | 0.62 | 130 | 114 | <1 | <5 | <0.1 | 0.5 | 183 | 77.1 | 1.8 | 3.1 | 1.21 | 2.26 | 6 | 5.74 | <1 | 3 | 0.51 | <0.2 | 107 |
| 17VEN-CRD-SampleA | 0.49 | 98 | 56 | <1 | <5 | <0.1 | <0.2 | 112 | 79.7 | 3 | 2.63 | 1.24 | 1.52 | 8 | 4.11 | <1 | 3 | 0.46 | <0.2 | 64.9 |
| 17VEN-CRD-SampleB | 0.43 | 109 | 63 | <1 | <5 | 0.2 | <0.2 | 91 | 53.4 | 2.7 | 3.37 | 1.83 | 1.45 | 10 | 4.21 | 1 | 3 | 0.69 | <0.2 | 54.3 |
| 17VEN-CRD1-01A | 0.54 | 104 | 54 | 2 | <5 | <0.1 | <0.2 | 121 | 76.8 | 2.5 | 2.71 | 1.26 | 1.54 | 8 | 4.31 | 1 | 3 | 0.47 | <0.2 | 69.6 |
| 17VEN-FRD2-SampleA-Cycl | 0.47 | 109 | 76 | <1 | <5 | 0.2 | <0.2 | 93.9 | 58.6 | 3.3 | 4.38 | 2.74 | 1.32 | 11 | 4.55 | 1 | 4 | 0.88 | <0.2 | 51.6 |
| 17VEN-FRD1-06a | 0.44 | 114 | 96 | <1 | <5 | 0.2 | 0.2 | 88 | 56.6 | 3 | 3.65 | 1.84 | 1.34 | 12 | 4.51 | 1 | 3 | 0.67 | <0.2 | 50.4 |
| 17VEN-FRD2-11A | 0.37 | 87 | 76 | <1 | <5 | <0.1 | <0.2 | 85.5 | 70.2 | 3.4 | 2.18 | 1.02 | 1.13 | 9 | 3.21 | <1 | 2 | 0.39 | <0.2 | 49.3 |
| 17VEN-FRD2-12A | 0.38 | 86 | 71 | <1 | <5 | <0.1 | <0.2 | 86.8 | 72.1 | 3.6 | 2.14 | 1.02 | 1.12 | 9 | 3.23 | <1 | 2 | 0.39 | <0.2 | 49.4 |
| 17VEN-FRD2-13A | 0.35 | 86 | 69 | <1 | <5 | <0.1 | <0.2 | 77.2 | 72.7 | 3.5 | 2.14 | 1.13 | 1.02 | 9 | 3.07 | <1 | 2 | 0.39 | <0.2 | 44 |
| 17GK-21 | 0.36 | 42 | 49 | <1 | <5 | <0.1 | <0.2 | 161 | 92.9 | 0.7 | 1.77 | 0.55 | 1.67 | 6 | 4 | <1 | 2 | 0.26 | <0.2 | 97.1 |
| 17GK-22 | 0.33 | 92 | 39 | <1 | <5 | <0.1 | <0.2 | 175 | 82.3 | 0.5 | 1.62 | 0.55 | 1.68 | 4 | 3.91 | <1 | 2 | 0.26 | <0.2 | 91.4 |
| 17GK-23 | 0.36 | 101 | 56 | <1 | <5 | <0.1 | <0.2 | 164 | 84.6 | 1.1 | 1.88 | 0.63 | 1.61 | 6 | 4.02 | <1 | 2 | 0.27 | <0.2 | 100 |
| 17GK-J-24 | 0.31 | 54 | 21 | <1 | <5 | <0.1 | <0.2 | 148 | 58.7 | 0.4 | 1.72 | 0.58 | 1.51 | 9 | 3.94 | <1 | 3 | 0.26 | <0.2 | 84.2 |

Table S1. Continued

| Sample | Lu | Mo | Nb | Nd | Pb | Pr | Rb | Sb | Sm | Sn | Ta | Tb | Th | Tl | Tm | U | W | Y | Yb | Zr | LOI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | ppm | % |
| 17VEN-K1-KIMB1 | 0.18 | <2 | 109 | 45.6 | 5 | 13.6 | 78.1 | 0.1 | 6.3 | <1 | 6.2 | 0.5 | 12.5 | <0.5 | 0.18 | 3.44 | 9 | 10.1 | 0.8 | 82.6 | 13.1 |
| 17VEN-K1-KIMB2 | 0.1 | <2 | 149 | 50.7 | <5 | 15.12 | 79.2 | <0.1 | 7 | <1 | 9.4 | 0.53 | 13.7 | <0.5 | 0.12 | 2.98 | 7 | 9.6 | 0.7 | 86.1 | 12.7 |
| 17VEN-K1-KIMB3 | 0.13 | <2 | 104 | 42.4 | 6 | 12.43 | 105 | 0.1 | 5.8 | <1 | 5.9 | 0.47 | 13.2 | <0.5 | 0.13 | 2.78 | <1 | 9.5 | 0.8 | 84.8 | 9.33 |
| 17VEN-K2-KIMB1 | 0.17 | <2 | 63 | 28.7 | 15 | 8.23 | 60.1 | <0.1 | 4.6 | 1 | 3.3 | 0.45 | 8.8 | <0.5 | 0.17 | 2.48 | 7 | 11.9 | 1.2 | 81.3 | 10.2 |
| 17VEN-K2-KIMB2 | 0.22 | <2 | 101 | 43.4 | 34 | 12.74 | 127 | <0.1 | 6.5 | 2 | 4.9 | 0.62 | 15.1 | <0.5 | 0.23 | 3.75 | 7 | 15.4 | 1.3 | 95.5 | 12.7 |
| 17VEN-K3-KIMB1 | 0.12 | <2 | 116 | 44.8 | 6 | 12.78 | 120 | 0.1 | 6.3 | <1 | 5.7 | 0.5 | 13.4 | <0.5 | 0.14 | 2.93 | 8 | 11.2 | 0.9 | 86.8 | 10.4 |
| 17VEN-K3-KIMB2 | 0.23 | <2 | 121 | 49.8 | 7 | 14.25 | 122 | 0.2 | 7.2 | 1 | 6.1 | 0.67 | 13.7 | <0.5 | 0.24 | 3.01 | 11 | 17.3 | 1.5 | 107 | 8.67 |
| 17VEN-K3-KIMB3 | 0.15 | <2 | 92 | 37.2 | 11 | 11.2 | 140 | 0.1 | 5.8 | 1 | 4.4 | 0.52 | 12.2 | <0.5 | 0.19 | 3.14 | 8 | 13.5 | 1.1 | 90.8 | 8.36 |
| 17VEN-K3-KIMB4 | 0.12 | <2 | 168 | 62.6 | 10 | 18.37 | 105 | 0.2 | 8.8 | 1 | 8.5 | 0.65 | 18.1 | <0.5 | 0.15 | 4.45 | 11 | 13.2 | 0.9 | 96.8 | 12.2 |
| 17VEN-CRD-SampleA | 0.14 | <2 | 106 | 40.2 | 10 | 11.73 | 84.9 | 0.1 | 5.9 | 1 | 5.8 | 0.51 | 11.6 | <0.5 | 0.17 | 2.8 | 18 | 12.5 | 1 | 103 | 11.6 |
| 17VEN-CRD-SampleB | 0.27 | <2 | 65 | 34 | 21 | 9.97 | 75.5 | 0.9 | 5.5 | 2 | 3.6 | 0.63 | 10.5 | 0.7 | 0.28 | 2.52 | 18 | 16.8 | 1.7 | 103 | 8.29 |
| 17VEN-CRD1-01A | 0.14 | <2 | 110 | 44 | 9 | 12.69 | 87 | 0.1 | 6.3 | 1 | 6.6 | 0.53 | 13.5 | <0.5 | 0.18 | 3.07 | 14 | 12.4 | 1 | 88.1 | 11.2 |
| 17VEN-FRD2-SampleA-Cycl | 0.41 | <2 | 56 | 35.9 | 12 | 10.14 | 86.7 | 0.2 | 5.6 | 2 | 3.1 | 0.72 | 12.9 | <0.5 | 0.42 | 3.45 | 3 | 24.8 | 2.8 | 157 | 7.93 |
| 17VEN-FRD1-06a | 0.25 | <2 | 63 | 33.1 | 16 | 9.42 | 94.2 | <0.1 | 5.6 | 2 | 3.4 | 0.66 | 12.3 | <0.5 | 0.27 | 4.5 | 1 | 18.4 | 1.7 | 102 | 7.7 |
| 17VEN-FRD2-11A | 0.13 | 8 | 70 | 31 | 11 | 8.88 | 78.7 | <0.1 | 4.5 | 1 | 3.9 | 0.42 | 9.6 | <0.5 | 0.15 | 2.57 | 1 | 10.6 | 0.9 | 85.4 | 12.9 |
| 17VEN-FRD2-12A | 0.13 | 7 | 72 | 31.2 | 11 | 9.02 | 83.8 | 0.1 | 4.5 | 1 | 3.8 | 0.41 | 10.3 | <0.5 | 0.14 | 2.56 | 1 | 10.4 | 0.8 | 72.6 | 12.7 |
| 17VEN-FRD2-13A | 0.15 | 3 | 62 | 28 | 11 | 8.08 | 76.8 | <0.1 | 4.1 | 1 | 3.2 | 0.41 | 9.3 | <0.5 | 0.15 | 2.56 | 1 | 10.7 | 0.9 | 73.8 | 12.6 |
| 17GK-21 | <0.05 | <2 | 109 | 52.8 | 12 | 16.43 | 74.9 | <0.1 | 6.8 | <1 | 6.2 | 0.45 | 15.7 | <0.5 | 0.06 | 2.32 | 5 | 6.7 | 0.3 | 60 | 11.4 |
| 17GK-22 | <0.05 | <2 | 114 | 58.5 | <5 | 18.11 | 37.6 | 0.1 | 7.1 | <1 | 5.6 | 0.43 | 15 | <0.5 | 0.07 | 2.7 | 3 | 6.7 | 0.3 | 70.6 | 15.6 |
| 17GK-23 | 0.05 | <2 | 120 | 53.3 | 13 | 16.38 | 103 | 0.2 | 7 | <1 | 6.5 | 0.43 | 15.3 | <0.5 | 0.07 | 2.53 | 10 | 7 | 0.4 | 66.8 | 11.2 |
| 17GK-J-24 | 0.06 | <2 | 90 | 51.6 | <5 | 15.4 | 57.6 | <0.1 | 6.9 | <1 | 4.6 | 0.43 | 17.9 | <0.5 | 0.07 | 1.91 | 3 | 6.5 | 0.4 | 92.3 | 14.8 |

Table S1. Continued

| Sample | SiO2 | Al2O3 | Fe2O3 | MgO | CaO | K2O | Na2O | TiO2 | MnO | P2O5 | Cr2O3 | V2O5 | Sum |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | % | % | % | % | % | % | % | % | % | % | % | % | % |
| 17VEN-K1-KIMB1 | 35.1 | 4.18 | 8.67 | 28.2 | 7.06 | 1.81 | 0.18 | 1.03 | 0.14 | 0.39 | 0.22 | 0.02 | 100.1 |
| 17VEN-K1-KIMB2 | 35 | 3.44 | 7.95 | 29.4 | 7.72 | 1.75 | 0.15 | 1.02 | 0.12 | 0.41 | 0.22 | 0.01 | 99.9 |
| 17VEN-K1-KIMB3 | 39.9 | 4.28 | 8.09 | 27 | 7.46 | 2.53 | 0.38 | 0.89 | 0.15 | 0.32 | 0.21 | 0.01 | 100.6 |
| 17VEN-K2-KIMB1 | 42.1 | 5.69 | 8.84 | 21.8 | 8.19 | 1.02 | 1.12 | 0.69 | 0.17 | 0.24 | 0.12 | 0.02 | 100.2 |
| 17VEN-K2-KIMB2 | 39 | 6.72 | 7.85 | 20 | 8.74 | 2.26 | 1 | 0.88 | 0.18 | 0.38 | 0.12 | 0.02 | 99.8 |
| 17VEN-K3-KIMB1 | 37.3 | 4.54 | 7.86 | 26.9 | 8.78 | 2.23 | 0.19 | 0.79 | 0.19 | 0.44 | 0.16 | 0.02 | 99.7 |
| 17VEN-K3-KIMB2 | 37.8 | 5.38 | 9.41 | 24.4 | 9.51 | 2.24 | 0.56 | 1.07 | 0.19 | 0.45 | 0.16 | 0.03 | 99.9 |
| 17VEN-K3-KIMB3 | 40.3 | 5.77 | 8.29 | 22.6 | 8.74 | 3.11 | 1.15 | 0.78 | 0.2 | 0.35 | 0.13 | 0.02 | 99.8 |
| 17VEN-K3-KIMB4 | 34.4 | 3.31 | 9.32 | 28 | 9.59 | 1.21 | 0.07 | 1.06 | 0.24 | 0.6 | 0.19 | 0.03 | 100.2 |
| 17VEN-CRD-SampleA | 40.1 | 4.97 | 8.01 | 24.8 | 7.1 | 1.75 | 0.86 | 0.84 | 0.14 | 0.34 | 0.16 | 0.02 | 100.7 |
| 17VEN-CRD-SampleB | 46.2 | 7.86 | 7.84 | 17.4 | 7.81 | 1.85 | 1.67 | 0.8 | 0.14 | 0.27 | 0.11 | 0.02 | 100.3 |
| 17VEN-CRD1-01A | 39.3 | 5.02 | 8.18 | 24.9 | 7.36 | 1.93 | 0.77 | 0.91 | 0.14 | 0.37 | 0.17 | 0.02 | 100.3 |
| 17VEN-FRD2-SampleA-Cycl | 47.8 | 8.02 | 7.98 | 17.4 | 6.13 | 2.19 | 1.41 | 0.81 | 0.14 | 0.24 | 0.12 | 0.02 | 100.1 |
| 17VEN-FRD1-06a | 48.2 | 8.71 | 7.94 | 15.2 | 7.23 | 2.21 | 1.54 | 0.75 | 0.17 | 0.25 | 0.1 | 0.03 | 100 |
| 17VEN-FRD2-11A | 39.3 | 6.09 | 7.74 | 22.7 | 6.56 | 1.59 | 2.1 | 0.65 | 0.13 | 0.27 | 0.12 | 0.02 | 100.3 |
| 17VEN-FRD2-12A | 39.4 | 6.04 | 7.76 | 23.2 | 6.64 | 1.59 | 1.66 | 0.64 | 0.13 | 0.28 | 0.11 | 0.01 | 100.1 |
| 17VEN-FRD2-13A | 40.7 | 6.15 | 7.78 | 22.7 | 6.37 | 1.37 | 1.56 | 0.6 | 0.13 | 0.23 | 0.11 | <0.01 | 100.3 |
| 17GK-21 | 38.5 | 3.03 | 7.72 | 30.8 | 5.82 | 1.47 | 0.36 | 0.6 | 0.13 | 0.35 | 0.23 | 0.01 | 100.4 |
| 17GK-22 | 37.3 | 2.6 | 7.22 | 35 | 1.24 | 0.45 | 0.07 | 0.55 | 0.14 | 0.36 | 0.22 | 0.02 | 100.8 |
| 17GK-23 | 39.1 | 3 | 8 | 31.4 | 4.17 | 1.78 | 0.38 | 0.62 | 0.14 | 0.42 | 0.24 | 0.02 | 100.5 |
| 17GK-J-24 | 44.2 | 5.95 | 5.95 | 25.2 | 1.38 | 1.62 | 0.32 | 0.53 | 0.04 | 0.21 | 0.17 | 0.01 | 100.4 |

Table S2. Cation Exchange Capacity and BET surface area

| Sample | Pulverized | BET | Cations measured in the NH4-Ac. leachates by ICP-AES |  |  |  |  |  |  | Normalized to 1 kg of rock |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Na | Mg | K | Ca | Mn | Fe | Al | Na | Mg | K | Ca |
|  |  | m2/g | mg/L | mg/L | mg/L | mg/L | mg/L | mg/L | mg/L | g/kg | g/kg | g/kg | g/kg |
| 17VEN-K1-KIMB1 | ✓ | 23.35 | 21.26 | 70.89 | 28.54 | 362.35 | 0.04 | 0.01 | 0.05 | 0.53 | 1.77 | 0.71 | 9.06 |
| 17VEN-K1-KIMB2 | ✓ | 11.19 | 9.41 | 44.43 | 11.99 | 327.57 | 0.07 | 0.00 | 0.07 | 0.24 | 1.11 | 0.30 | 8.19 |
| 17VEN-K1-KIMB3 | ✓ | 12.42 | 23.73 | 34.12 | 16.83 | 182.56 | 0.29 | 0.11 | 0.02 | 0.59 | 0.85 | 0.42 | 4.56 |
| 17VEN-K2-KIMB1 | ✓ | 19.34 | 112.77 | 22.26 | 18.35 | 281.20 | 0.04 | 0.02 | 0.03 | 2.82 | 0.56 | 0.46 | 7.03 |
| 17VEN-K2-KIMB2 | ✓ | 20.11 | 157.24 | 20.80 | 27.89 | 417.01 | 0.07 | 0.01 | 0.03 | 3.93 | 0.52 | 0.70 | 10.43 |
| 17VEN-K3-KIMB1 | ✓ | 17.10 | 23.34 | 36.20 | 16.43 | 323.49 | 0.13 | 0.00 | <0.008 | 0.58 | 0.90 | 0.41 | 8.09 |
| 17VEN-K3-KIMB2 | ✓ | 15.16 | 20.33 | 62.36 | 22.97 | 145.24 | 0.16 | 0.01 | 0.02 | 0.51 | 1.56 | 0.57 | 3.63 |
| 17VEN-K3-KIMB3 | ✓ | 14.09 | 58.18 | 21.03 | 33.77 | 286.80 | 0.08 | 0.00 | 0.02 | 1.45 | 0.53 | 0.84 | 7.17 |
| 17VEN-K3-KIMB4 | ✓ | 10.07 | 9.28 | 55.72 | 9.84 | 321.02 | 0.28 | 0.02 | 0.04 | 0.23 | 1.39 | 0.25 | 8.03 |
| 17VEN-CRD-sampleA | ✓ | 25.31 | 69.79 | 66.26 | 56.67 | 334.85 | 0.07 | 0.01 | 0.03 | 1.74 | 1.66 | 1.42 | 8.37 |
| 17VEN-CRD-SampleB | ✓ | 12.46 | 66.90 | 21.79 | 25.70 | 325.26 | 0.10 | 0.01 | 0.02 | 1.67 | 0.54 | 0.64 | 8.13 |
| 17VEN-CRD-SampleB | X | 6.09 | 52.51 | 3.18 | 12.59 | 61.10 | 0.03 | 0.02 | 0.01 | 1.31 | 0.08 | 0.31 | 1.53 |
| 17VEN-CRD1-01A | ✓ | 18.76 | 49.04 | 62.07 | 38.05 | 356.19 | 0.05 | 0.01 | 0.02 | 1.23 | 1.55 | 0.95 | 8.90 |
| 17VEN-FRD2-SampleA-Cycl | ✓ | 12.19 | 108.69 | 15.87 | 25.87 | 259.79 | 0.26 | 0.01 | 0.01 | 2.72 | 0.40 | 0.65 | 6.49 |
| 17VEN-FRD1-06a | ✓ | 7.61 | 100.30 | 13.25 | 17.70 | 233.82 | 0.37 | 0.01 | 0.02 | 2.51 | 0.33 | 0.44 | 5.85 |
| 17VEN-FRD2-11A | ✓ | 17.41 | 505.04 | 15.30 | 63.83 | 358.85 | 0.05 | <0.001 | 0.02 | 12.63 | 0.38 | 1.60 | 8.97 |
| 17GK-21 | ✓ | 14.68 | 3.11 | 85.46 | 12.96 | 118.48 | 0.06 | 0.02 | 0.02 | 0.08 | 2.14 | 0.32 | 2.96 |
| 17GK-22 | ✓ | 44.97 | 1.12 | 84.19 | 3.73 | 69.41 | 0.07 | 0.03 | <0.008 | 0.03 | 2.10 | 0.09 | 1.74 |
| 17GK-23 | ✓ | 14.76 | 4.36 | 42.62 | 14.28 | 67.10 | 0.06 | <0.001 | 0.01 | 0.11 | 1.07 | 0.36 | 1.68 |
| 17GK-J-24 | ✓ | 44.57 | 7.87 | 95.30 | 9.18 | 269.41 | 0.03 | 0.01 | <0.008 | 0.20 | 2.38 | 0.23 | 6.74 |

Table S2. Continued

| Sample | Cations measured in the NH4-Ac. leachates by ICP-AES |  |  |  |  |  |  | BET corrected |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Na | Mg | K | Ca | Mn | Fe | Al | Na | Mg | K | Ca |
|  | cmol(+)/kg | cmol(+)/kg | cmol(+)/kg | cmol(+)/kg | cmol(+)/kg | cmol(+)/kg | cmol(+)/kg | cmol(+)/m2 | cmol(+)/m2 | cmol(+)/m2 | cmol(+)/m2 |
| 17VEN-K1-KIMB1 | 2.31 | 14.59 | 1.83 | 45.29 | 0.00 | 0.00 | 0.01 | 0.00010 | 0.00062 | 0.00008 | 0.00194 |
| 17VEN-K1-KIMB2 | 1.02 | 9.14 | 0.77 | 40.95 | 0.01 | 0.00 | 0.02 | 0.00009 | 0.00082 | 0.00007 | 0.00366 |
| 17VEN-K1-KIMB3 | 2.58 | 7.02 | 1.08 | 22.82 | 0.03 | 0.00 | 0.01 | 0.00021 | 0.00057 | 0.00009 | 0.00184 |
| 17VEN-K2-KIMB1 | 12.26 | 4.58 | 1.17 | 35.15 | 0.00 | 0.00 | 0.01 | 0.00063 | 0.00024 | 0.00006 | 0.00182 |
| 17VEN-K2-KIMB2 | 17.10 | 4.28 | 1.79 | 52.13 | 0.01 | 0.00 | 0.01 | 0.00085 | 0.00021 | 0.00009 | 0.00259 |
| 17VEN-K3-KIMB1 | 2.54 | 7.45 | 1.05 | 40.44 | 0.01 | 0.00 | 0.00 | 0.00015 | 0.00044 | 0.00006 | 0.00236 |
| 17VEN-K3-KIMB2 | 2.21 | 12.83 | 1.47 | 18.15 | 0.01 | 0.00 | 0.01 | 0.00015 | 0.00085 | 0.00010 | 0.00120 |
| 17VEN-K3-KIMB3 | 6.33 | 4.33 | 2.16 | 35.85 | 0.01 | 0.00 | 0.00 | 0.00045 | 0.00031 | 0.00015 | 0.00254 |
| 17VEN-K3-KIMB4 | 1.01 | 11.47 | 0.63 | 40.13 | 0.03 | 0.00 | 0.01 | 0.00010 | 0.00114 | 0.00006 | 0.00398 |
| 17VEN-CRD-sampleA | 7.59 | 13.63 | 3.63 | 41.86 | 0.01 | 0.00 | 0.01 | 0.00030 | 0.00054 | 0.00014 | 0.00165 |
| 17VEN-CRD-SampleB | 7.28 | 4.48 | 1.64 | 40.66 | 0.01 | 0.00 | 0.01 | 0.00058 | 0.00036 | 0.00013 | 0.00326 |
| 17VEN-CRD-SampleB | 5.71 | 0.65 | 0.81 | 7.64 | 0.00 | 0.00 | 0.00 | 0.00094 | 0.00011 | 0.00013 | 0.00125 |
| 17VEN-CRD1-01A | 5.33 | 12.77 | 2.44 | 44.52 | 0.00 | 0.00 | 0.00 | 0.00028 | 0.00068 | 0.00013 | 0.00237 |
| 17VEN-FRD2-SampleA-Cycl | 11.82 | 3.27 | 1.66 | 32.47 | 0.02 | 0.00 | 0.00 | 0.00097 | 0.00027 | 0.00014 | 0.00266 |
| 17VEN-FRD1-06a | 10.91 | 2.73 | 1.13 | 29.23 | 0.03 | 0.00 | 0.00 | 0.00143 | 0.00036 | 0.00015 | 0.00384 |
| 17VEN-FRD2-11A | 54.92 | 3.15 | 4.08 | 44.86 | 0.00 | 0.00 | 0.00 | 0.00315 | 0.00018 | 0.00023 | 0.00258 |
| 17GK-21 | 0.34 | 17.58 | 0.83 | 14.81 | 0.01 | 0.00 | 0.01 | 0.00002 | 0.00120 | 0.00006 | 0.00101 |
| 17GK-22 | 0.12 | 17.32 | 0.24 | 8.68 | 0.01 | 0.00 | 0.00 | 0.00000 | 0.00039 | 0.00001 | 0.00019 |
| 17GK-23 | 0.47 | 8.77 | 0.91 | 8.39 | 0.01 | 0.00 | 0.00 | 0.00003 | 0.00059 | 0.00006 | 0.00057 |
| 17GK-J-24 | 0.86 | 19.61 | 0.59 | 33.68 | 0.00 | 0.00 | 0.00 | 0.00002 | 0.00044 | 0.00001 | 0.00076 |

Table S2. Continued

| Sample | CEC (cations) |  | CEC (NH4-N) |  |  |
| --- | --- | --- | --- | --- | --- |
|  | CEC-cations | CEC-cations (BET norm.) | NH4-N |  | CEC-NH4-N (BET norm.) |
|  | cmol(+)/kg | cmol(+)/m2 | mg/L | cmol(+)/kg | cmol(+)/m2 |
| 17VEN-K1-KIMB1 | 64.03 | 0.0027 | 40.67 | 7.263 | 0.00031 |
| 17VEN-K1-KIMB2 | 51.90 | 0.0046 | 23.72 | 4.236 | 0.00038 |
| 17VEN-K1-KIMB3 | 33.54 | 0.0027 | 29.61 | 5.287 | 0.00043 |
| 17VEN-K2-KIMB1 | 53.18 | 0.0028 | 153.78 | 27.462 | 0.00142 |
| 17VEN-K2-KIMB2 | 75.31 | 0.0037 | 197.66 | 35.297 | 0.00175 |
| 17VEN-K3-KIMB1 | 51.49 | 0.0030 | 48.29 | 8.624 | 0.00050 |
| 17VEN-K3-KIMB2 | 34.69 | 0.0023 | 39.32 | 7.021 | 0.00046 |
| 17VEN-K3-KIMB3 | 48.68 | 0.0035 | 61.38 | 10.961 | 0.00078 |
| 17VEN-K3-KIMB4 | 53.27 | 0.0053 | 20.82 | 3.719 | 0.00037 |
| 17VEN-CRD-sampleA | 66.72 | 0.0026 | 100.80 | 18.000 | 0.00071 |
| 17VEN-CRD-SampleB | 54.08 | 0.0043 | 68.86 | 12.296 | 0.00099 |
| 17VEN-CRD-SampleB | 14.81 | 0.0024 | 14.01 | 2.502 | 0.00041 |
| 17VEN-CRD1-01A | 65.07 | 0.0035 | 63.43 | 11.327 | 0.00060 |
| 17VEN-FRD2-SampleA-Cycl | 49.24 | 0.0040 | 144.25 | 25.759 | 0.00211 |
| 17VEN-FRD1-06a | 44.03 | 0.0058 | 122.01 | 21.788 | 0.00286 |
| 17VEN-FRD2-11A | 107.02 | 0.0061 | 182.84 | 32.651 | 0.00188 |
| 17GK-21 | 33.57 | 0.0023 | 28.91 | 5.162 | 0.00035 |
| 17GK-22 | 26.37 | 0.0006 | 35.23 | 6.291 | 0.00014 |
| 17GK-23 | 18.55 | 0.0013 | 38.81 | 6.930 | 0.00047 |
| 17GK-J-24 | 54.73 | 0.0012 | 281.72 | 50.307 | 0.00113 |

FIGURES

Fig. S1. Rietveld refinement plot for kimberlite ore sample, 17VEN-K2-KIMB1 (MVK facies). X-ray diffraction data (blue curve), the modelled fit to the data (red), residual intensity (grey) and fits to individual mineral phases (colors as marked in the legend) are displayed. The positions of Bragg peaks for each phase employed in the model are indicated as short vertical lines beneath the observed and modelled XRD patterns. The Rwp of this refinement is 7.5%.

Fig. S2. Example TGA and derivative thermogravimetry (DTG) analyses for (A) one sample from Gahcho Kué and (B) and (C) two samples from Venetia.

Fig. S3. ATR-FTIR spectra of 17VEN-K1-KIMB2 ore (facies CKNE/MVK Contact kimberlite; K1 Pit), 17VEN-FRD2-12A (crust from FRD2, likely MVK facies) and 17GK-J-24 ore (J; TKt; West Lobe): (A) Mid-IR region and (B) OH-stretching region. Mineralogy: P: phlogopite, L: lizardite, C: calcite, D: diopside, Cl: clinochlore, T: talc, S: saponite.

Fig. S4. Diagrams of smectite content of the samples (wt.%) versus individual exchangeable cations (A) Na (B) K and (C) Mg and (D) Ca contents (cmol(+)/m2) in the NH4-acetate leachates. No significant correlations are observed.

Fig. S5. Calcite distribution (indicated by white arrows) within four different facies from Venetia: (A) CKNE; (B) CKNE/MVK; (C) DVK; (D) VK.

REFERENCES

Cheary, R.W., and Coelho, A. A., 1998, Axial Divergence in a Conventional X-ray Powder Diffractometer. II. Realization and Evaluation in a Fundamental-Parameter Profile Fitting Procedure: Journal of Applied Crystallography, v. 31, p. 862–868.

Dollase, W., 1986, Correction of intensities for preferred orientation in powder diffractometry: Application of the March model: Journal of Applied Crystallography, v. 19(4), p. 267–272.

March, A., 1932, Mathematische theorie der regelung nach der korn gestalt bei affiner deformation: Zeitschrift für Kristallographie, v. 81, p. 285–297.

Mellini, M., Viti, C., 1994, Crystal structure of lizardite-1T from Elba, Italy: American Mineralogist, v. 79(11-12), p. 1194–1198.

O’Gorman, J.V., and Kitchener, J.A., 1974, The flocculation and de-watering of kimberlite clay slimes: International Journal of Mineral Processing, v. 1, p. 33–49.

Pawley, G.S., 1981, Unit-cell refinement from powder diffraction scans: Journal of Applied Crystallography, v. 14, p. 357–361.

Scarlett, N.V.Y., and Madsen, I.C., 2006, Quantification of phases with partial or no known crystal structures: Powder Diffraction, v. 21, p. 278–284.

Viani, A., Gualtieri, A.F., and Artioli, G., 2002, The nature of disorder in montmorillonite by simulation of X-ray powder patterns: American Mineralogist, v. 87, p. 966–975.

Wang, B., Zeyen, N., Wilson, S.A., Funk, R., and Turvey C.C., Quantifying the potential for mineral carbonation of processed kimberlite with the Rietveld-PONKCS method. In Prep.